## Slide 1: Design of O-Ring Seals

## Slide 2: Design of O-Ring Seals
Primary Source of information

## Slide 3: Why O-Rings?
  Can be used for static and dynamic applications
  Compact – need very little space - light weight
  Easy to incorporate into design
  Do not require high accuracy
  Simple design rules
  Easy to install or remove
  Easy to service
  Available in many standard sizes, materials

## Slide 4: Why O-Rings?
  Wide range of operating temperatures
  Wide range of operating pressures
  Good durability and abrasion resistance
  O-ring materials for a wide range of chemicals
  Their failure or deterioration is gradual
  Inexpensive

## Slide 5: Limitations of O-rings
Temperature (typically between -40 and 400 degrees F)
Rotary speeds ( not to exceeding 1500 feet per minute)
  For a 2 inch shaft, it is 3000 rpm
Vulnerable to sharp edges
Require small clearances

## Slide 6: O-Rings

## Slide 7: Popular O-ring materials
Nitrile (Buna-N)
  Variety of trade names
  Copolymer of butadiene and acrylonitrile
  Most widely used and economical elastomer
  Temperature Range: Standard Compound: -40° to +257°F
  Hardness (Shore A): 40 to 90

## Slide 8: Popular O-ring materials Nitrile (Buna-N)
Excellent resistance to
  petroleum-based oils and fuels
  silicone greases
  hydraulic fluids
  water and alcohol
High tensile strength
High abrasion resistance

## Slide 9: Popular O-ring materials Nitrile (Buna-N)
Applications
  Oil resistant applications
  Low temperature uses
  Off-road equipment
  Automotive, marine, aircraft fuel systems

## Slide 10: Other O-ring Materials
Viton® / FKM: Fluorocarbon (Viton®) exceptional resistance to chemicals, oils, temperature extremes (-13°F to +446°F), low compression set. Applications include: aircraft engines, automotive fuel handling systems, and chemical processing industries.
Ethylene-Propylene / EPDM: EPDM has excellent resistance to heat, water and steam, alkali, mild acidic and solvents, ozone, and sunlight with a temperature range of (-40ºF to +275ºF); but it is not recommended for gasoline, petroleum oil and grease, and hydrocarbon environments.

## Slide 11: Other O-ring Materials
Fluorosilicone / FVMQ: Fluorosilicone (-75º to +400ºF) combines the good high and low temperature stability of silicones with the fuel, oil, and solvent resistance of fluorocarbons. FVMQ is used for aerospace fuel systems, auto fuel emission control systems. However, due to relatively low tear strength, high friction and limited abrasion resistance of these materials, they are generally not used in dynamic applications.

## Slide 12: Other O-ring Materials
Silicone / VMQ: Superior as static seals in extreme temperature conditions. Standard compounds handle operating temperatures -85º to +400ºF. Silicone compounds are popular in food and medical applications because they are clean and do not impart odor or taste. Special Phenyl silicones can be used down to -148°F.

## Slide 13: Other O-ring Materials
Neoprene® / CR: Neoprene (-40º to +250ºF) features good resistance to petroleum oils, ozone, sunlight, relatively low compression set, good resilience and physical toughness. It is the preferred sealing material for the refrigeration industry because of its resistance to ammonia and Freon

## Slide 17: O-Ring Seal Design
The O-ring Specifications
  Size (inside diameter)
    1/32 to 26 inches
  CS (Cross-Section)
    1/32 to ¼ inch
  Rigidity (Hardness)
  Material

## Slide 18: O-ring Standards
Standard
  AS568
  ISO 3601
Example
  AS016-70N Nitrile O-ring
  (AS568-016 Size 0.070 CS x 0.614 ID)

## Slide 19: O-ring Search Tools

## Slide 21: O-Ring Hardness
Measured on Shore-A hardness index
  Shore 20A = Rubber Band
  Shore 40A = Pencil Eraser
  Shore 60A = Car Tire Tread
  Shore 70A* = Running Shoe Sole
  Shore 80A = Leather Belt
  Shore 100A = Shopping Cart Wheel

## Slide 23: O-Ring Properties
Fluid resistance
Hardness
Toughness
Volume change (swell / shrinkage)
Compression set
Thermal effects
Resilience
Deterioration
Corrosion
Permeability
Coefficient of friction
Coefficient of thermal expansion
Compression set relaxation
Tensile strength
Elongation
Tear resistance / Abrasion resistance

## Slide 24: O-ring Seal Design
The Gland (Groove + Spacing)
  Depth of groove
  Width of groove
  Diameter of bore and piston
  Surface finish
  Tolerances

## Slide 25: Static Seals
Static Axial Seal
(Face Seal)

## Slide 26: Static Seals
Static Crush Seal

## Slide 27: Static Seals
Static Radial Seal
(Piston Seal)

## Slide 28: Dynamic Seals
Reciprocating Seals

## Slide 29: Dynamic Seals
Rotary Seals

## Slide 30: Dynamic Seals

## Slide 31: General Design Guidelines
Stretch should be less than 5% on the O-ring I.D.
Groove depth must be smaller than the O-ring CS
O-ring should not completely fill the gland
  Between 75% and 90%
Static seal CS should be compressed from 10% to 40%
Dynamic seals should be compressed from 10% to 30%

## Slide 33: Design of Axial Seal
Axial Seal

## Slide 35: Example Design
Design a groove for a 1.5 inch diameter Internal pressure O-ring
  O-ring : -029 (ID: 1.489 +/- .013) (W: .07 +/- .003)
  Material: Buna-N
  Hardness: 70 Shore-A
  A: 1.624 (-0 , + .005)
  G: .125 (-0, + .01)
  H: .049 (-0,+.005)

## Slide 36: Example Design
Checking resulting compression
  Compression (squeeze) = W - H
  Min. Comp. = Wmin - Hmax
  Min. Comp. = 0.013 in (18.5%)
  Max. Comp. = Wmax - Hmin
  Max. Comp. = 0.024 in (34.3%)

## Slide 37: Radial Seal
Radial Static
Piston Seal

## Slide 38: Example Design
Design a groove for a 0.7 inch diameter piston ring
  O-ring : -029 (ID: .614 +/- .009) (W: .07 +/- .003)
  Material: Buna-N
  Hardness: 70 Shore-A
  A: .746 (-0 , + .002)
  B: .745 (-.001, + 0)
  C: .638 (-.001,+ 0)

## Slide 39: Example Design
Checking compression
  Comp = W – 0.5(A - C)
  Min. Comp = Wmin – 0.5(Amax – Cmin)
  Min. Comp. = 0.0115 in (17.1%)
  Max. Comp. = 0.024 in (26.0%)
Also check
  Extrusion gap
  Stretch
  Squeeze

## Slide 41
Radial Static
Rod Seal

## Slide 42
Static Crush Seal

## Slide 43
Static Crush Seal

## Slide 44: Dynamic Seals

## Slide 45: Gland Design For Dynamic O-ring Seals

## Slide 46: Reciprocating Motion

## Slide 47
The O-ring’s O.D. is larger than the cylinder bore diameter. Peripheral squeeze is applied to the O.D. as the O-ring is installed into the bore. Incoming air pressure forces the O-ring against the walls sealing

## Slide 48: Floating O-Rings
Advantage
  Greatly reduced breakout friction
  Longer seal life
Limitations
  Air pressure less than 200 psi in pneumatic cylinders
  In hydraulic systems small amount of leakage must be permissible
  Floating O-rings are NOT suitable as rod seals

## Slide 49: Alternatives to O-Rings U-cup Seals
O-rings have a tendency to roll and move in reciprocating motions
U-cups create more sealing as the pressure increases
U-cups require less precision for the associated hardware

## Slide 50: Alternatives to O-Rings U-cup Seals

## Slide 51: Typical Applications

## Slide 52: Buffer Seal
  Buffer seals are one-way seals that protect rod seals from pressure spikes yet allow fluid (lubricant) to reach the main seal

## Slide 53: Rotary Seals

## Slide 54: Due to centrifugal force and Gough-Joule effect rotary O-rings are only installed in the housing not on the shaft

## Slide 55: Gough-Joule effect
When an elastomer is stretched and heated, it will contract.

## Slide 56: Rotary O-Ring Limitations
O-ring seals are NOT recommended for rotary applications under the following conditions:
  Pressures exceeding 900 psi
  Temperatures lower than -40° F or higher than 225° F
  Surface speeds exceeding 600 feet per minute (fpm).
        2300 rpm for 1 inch diameter shaft
        1150 rpm for 2 inch diameter shaft

## Slide 57: Rotary Seals

## Slide 58: Lip Seals
Lip seals work well in high speed low pressure rotating shafts

## Slide 59: Main Application of Lip Seals
Ball and roller bearing protection
  As little as 0.002% water in lubrication oil can reduce ball bearing life by 50%
  Solid particles cause rapid damage to the bearing races.

## Slide 62
The purpose of the spring is to provide a uniform load on the lip
The spring keeps the seal lip in contact with the shaft during higher speeds and also overcomes compression set and wear of the lip material.

## Slide 63
There is a tendency for liquids to be pumped from the low angle side towards the high angle side. Underneath the flattened area a thin fluid film is formed. Its thickness must be between 1 and 3 µm to avoid leakage

## Slide 65
Primary function is retention
Primary function is exclusion

## Slide 68: Lip Seals
To minimize wear
  The contact pressure should be as low as possible.
  Shaft surface should be smooth to 0.25- 0.5µm.
  There must be enough fluid to form a hydrodynamic film
  Fluid pressure must be low (0-3 psi )

## Slide 69: V-Seals

## Slide 70: Flexi-Lip Rotary Seals
Speeds up to 5000 fps
Pressures up to 150 psi
Material: PTFE, graphite

## Slide 76: Metallic Seals
Metallic seals go where polymers cannot
  High temperatures (Above 400 to 1800 Degree F)
  Cryogenic temperatures (below −238 °F)
  High pressures (3000 psi to 60000 psi)
  High speeds

## Slide 77: Metal Seals

## Slide 78: C-Ring and Energized C-Ring

## Slide 79: E-Ring and O-Ring

## Slide 80: U-Ring and Metal Wire

## Slide 81: Combustion Engine Piston Rings
First compression ring (1)
Second compression ring (2)
Oil scraper ring (3)

## Slide 82: Piston Rings
Compression ring
  Seals the gases in the cylinder
  Gas pressure forces the ring against the cylinder wall
Wiper ring (secondary compression ring)
  Seals the gases that escape the compression ring
  Wipes excess oil from cylinder wall
Oil ring
  Made of two thin rails with slots
  Wipes excess oil from cylinder walls through port holes

## Slide 83: Labyrinth Seals

## Slide 84
Labyrinth Seal

## Slide 85
Labyrinth Seal

## Slide 86
Mechanical Seals
Rotating Elements