## Slide 1: Design of Seals

## Slide 2: Design of O-Ring Seals
Primary Source of information

## Slide 3: Why O-Rings?
  Static and dynamic applications
  Compact
  Easy to use
  Simple design rules
  Easy to install or remove
  Easy to service
  Available in many standard sizes, materials

## Slide 4: Why O-Rings?
  Wide range of operating temperatures
  Wide range of operating pressures
  Good durability and abrasion resistance
  Materials for a wide range of chemicals
  Deterioration is gradual
  Inexpensive

## Slide 5: Limitations of O-rings
Temperature (Typically -40 and 400 degrees F)
Rotary speeds ( not to exceeding 1500 feet per minute)
  For a 2 inch shaft, it is 3000 rpm
Vulnerable to sharp edges

## Slide 6: O-Rings

## Slide 7: Popular O-ring materials
Nitrile (Buna-N)
  Variety of trade names
  Copolymer of butadiene and acrylonitrile
  Most widely used and economical elastomer
  Temperature Range: -40° to +257°F
  Hardness (Shore A): 40 to 90

## Slide 8: Popular O-ring materials Nitrile (Buna-N)
Excellent resistance to
  petroleum-based oils and fuels
  silicone greases
  hydraulic fluids
  water and alcohol
High tensile strength
High abrasion resistance

## Slide 9: Popular O-ring materials Nitrile (Buna-N)
Applications
  Oil resistant applications
  Low temperature uses
  Off-road equipment
  Automotive, marine, aircraft fuel systems

## Slide 13: O-Ring Seal Design
The O-ring Specifications
  Size (inside diameter)
    1/32 to 26 inches
  CS (Cross-Section)
    1/32 to ¼ inch
  Rigidity (Hardness)
  Material

## Slide 14: O-ring Standards
Standard
  AS568
  ISO 3601
Example
  AS016-70N Nitrile O-ring
  (AS568-016 Size 0.070 CS x 0.614 ID)

## Slide 15: O-ring Search Tools

## Slide 17: O-Ring Hardness
Measured on Shore-A hardness index
  Shore 20A = Rubber Band
  Shore 40A = Pencil Eraser
  Shore 60A = Car Tire Tread
  Shore 70A* = Running Shoe Sole
  Shore 80A = Leather Belt
  Shore 100A = Shopping Cart Wheel

## Slide 19: O-Ring Properties
Fluid resistance
Hardness
Toughness
Volume change (swell / shrinkage)
Compression set
Thermal effects
Resilience
Deterioration
Corrosion
Permeability
Coefficient of friction
Coefficient of thermal expansion
Compression set relaxation
Tensile strength
Elongation
Tear resistance / Abrasion resistance

## Slide 20: O-ring Seal Design
The Gland (Groove + Spacing)
  Depth of groove
  Width of groove
  Diameter of bore and piston
  Surface finish
  Tolerances

## Slide 21: Static Seals
Static Axial Seal
(Face Seal)

## Slide 22: Static Seals
Static Crush Seal

## Slide 23: Static Seals
Static Radial Seal
(Piston Seal)

## Slide 24: Dynamic Seals
Reciprocating Seals

## Slide 25: Dynamic Seals
Rotary Seals

## Slide 26: Dynamic Seals

## Slide 27: General Design Guidelines
Stretch should be less than 5% on the O-ring I.D.

## Slide 28: Design Guidelines
Groove depth must be smaller than the O-ring CS

## Slide 29: Design Guidelines
O-ring should not completely fill the gland
  Between 75% and 90%
Static seal CS should be compressed from 10% to 40%
Dynamic seals should be compressed from 10% to 30%

## Slide 30: Design of Axial Seal
Axial Seal

## Slide 32: Example Design
Design a groove for a 1.5 inch diameter Internal pressure O-ring
  O-ring : -029 (ID: 1.489 +/- .013) (W: .07 +/- .003)
  Material: Buna-N
  Hardness: 70 Shore-A
  A: 1.624 (-0 , + .005)
  G: .125 (-0, + .01)
  H: .049 (-0,+.005)

## Slide 33: Example Design
Checking resulting compression
  Compression (squeeze) = W - H
  Min. Comp. = 0.013 in (18.5%)
  Max. Comp. = 0.024 in (34.3%)

## Slide 34: Radial Seal
Radial Static
Piston Seal

## Slide 35: Example Design
Design a groove for a 0.7 inch diameter piston ring
  O-ring : -029 (ID: .614 +/- .009) (W: .07 +/- .003)
  Material: Buna-N
  Hardness: 70 Shore-A
  A: .746 (-0 , + .002)
  B: .745 (-.001, + 0)
  C: .638 (-.001,+ 0)

## Slide 36: Example Design
Checking compression
  Comp = W – 0.5(A - C)
  Min. Comp. = 17.1%
  Max. Comp. = 26.0%
Also check
  Extrusion gap
  Stretch

## Slide 38
Radial Static
Rod Seal

## Slide 39
Static Crush Seal

## Slide 40
Static Crush Seal

## Slide 41: Dynamic Seals

## Slide 42: Reciprocating Motion

## Slide 44: Alternatives to O-Rings U-cup Seals
O-rings have a tendency to roll and move in reciprocating motions
U-cups create more sealing as the pressure increases
U-cups require less precision for the associated hardware

## Slide 45: Alternatives to O-Rings U-cup Seals

## Slide 46: Typical Applications

## Slide 47: Buffer Seal
  Buffer seals are one-way seals that protect rod seals from pressure spikes yet allow fluid (lubricant) to reach the main seal

## Slide 48: Rotary Seals

## Slide 49: Due to centrifugal force and Gough-Joule effect rotary O-rings are only installed in the housing not on the shaft

## Slide 50: Gough-Joule effect
When an elastomer is stretched and heated, it will contract.

## Slide 51: Rotary O-Ring Limitations
O-ring seals are NOT recommended for rotary applications under the following conditions:
  Pressures exceeding 900 psi
  Temperatures lower than -40° F or higher than 225° F
  Surface speeds exceeding 600 feet per minute (fpm).
        2300 rpm for 1 inch diameter shaft
        1150 rpm for 2 inch diameter shaft

## Slide 52: Rotary Seals

## Slide 53: Lip Seals
Lip seals work well in high speed low pressure rotating shafts

## Slide 54: Main Application of Lip Seals
Ball and roller bearing protection
  As little as 0.002% water in lubrication oil can reduce ball bearing life by 50%
  Solid particles cause rapid damage to the bearing races.

## Slide 57
The purpose of the spring is to provide a uniform load on the lip
Also overcomes compression set and wear of the lip material.

## Slide 58
There is a tendency for liquids to be pumped from the low angle side towards the high angle side. Underneath the flattened area a thin fluid film is formed. Its thickness must be between 1 and 3 µm to avoid leakage

## Slide 60
Primary function is retention
Primary function is exclusion

## Slide 63: Lip Seals
To minimize wear
  The contact pressure should be as low as possible.
  Shaft surface should be smooth to 0.25- 0.5 µm.
  There must be enough fluid to form a hydrodynamic film
  Fluid pressure must be low (0-3 psi )

## Slide 64: V-Seals

## Slide 65: Flexi-Lip Rotary Seals
Speeds up to 5000 fps
Pressures up to 150 psi
Material: PTFE, graphite

## Slide 71: Metallic Seals
Metallic seals go where polymers cannot
  High temperatures (Above 400 to 1800 Degree F)
  Cryogenic temperatures (below −238 °F)
  High pressures (3000 psi to 60000 psi)
  High speeds

## Slide 72: Metal Seals

## Slide 73: C-Ring and Energized C-Ring

## Slide 74: E-Ring and O-Ring

## Slide 75: U-Ring and Metal Wire

## Slide 76: Labyrinth Seals

## Slide 77
Labyrinth Seal

## Slide 78
Labyrinth Seal

## Slide 79
Mechanical Seals
Rotating Elements